| Parameter | Omnibus 4 | XD-4TM |  | Units |  |
| --- | --- | --- | --- | --- | --- |
|  | typical value’s | typical value’s |  |  |  |
| Signal to Noise ratio (108μlx) | 24 | 24 |  |  |  |
| Limiting resolution | 64 | 60 (68) |  | lp/mm | *1 |
| MTF (contrast) at: |  |  |  |  | *2 |
| 2,5 lp/mm | 90 | 92 |  | % |  |
| 7,5 lp/mm | 80 | 80 |  | % |  |
| 15 lp/mm | 61 | 68 |  | % |  |
| 25 lp/mm | 38 | 47 |  | % |  |
| 32 lp/mm |  | 37 |  | % |  |
| Luminance gain at 2.10-5 lx | 12000 – 22000 | 15000 |  | cd/m2/lx | *3 |
| E.B.I. (dark noise) | 0.15 | 0.15 |  | μlx |  |
| Wavelength band | 550 – 900 | 350 – 900 |  | nm |  |
| Life time | 10000 | 15000 |  | hours |  |
| Over illumination protection | vulnerable | good |  |  | *4 |
| Shock resistance | 75 | 500 |  | g’s |  |
| Halo size | ± 2.0 | ± 0.5 |  | mm | *5 |
| Gate voltage | 800 | 200 |  | V | *6 |
| Formats | 18 | 18 |  | mm |  |
| Export restrictions | US-export restricted | no US restrictions |  |  | *7 |

remarks:

- The European way of measuring limiting resolution is more conservative than how the Americans measure it. The value between brackets shows the value comparable with American measuring methods.

- The better contrast in the mid line-pair range has more contribution to a good overall performance than the absolute limiting resolution

- For gain in American units (fl/fc) the value’s have to be multiplied by pi (3.14)

- XD-4TM photocathodes are much less vulnerable to ion feedback than the GaAs photocathodes.

- The halo’s in XD-4TM tubes are not only smaller but also less intense.

- With a lower gate voltage faster gate times can be achieved.

- Because DEP does not rely on US ITAR components no DSP-83 form is required, which makes much faster delivery times possible.